## Slide 1: Superconducting magnet development for future high energy hadron colliders
Gijs de Rijk
10 January 2015
Epiphany conference
Krakow

## Slide 2: Contents
The aim: 16 T, 20 T ( and beyond ?) for high energy colliders
Conductors for high field accelerator magnets: needs and availability
The challenge beyond 10 T
Earliest preparation for HL-LHC: LARP
US dipole R&D
High Field Magnet development in Europe
High Field Magnets for HILUMI-HL-LHC
Fresca2
HTS magnet development: EuCARD and EuCARD2 inserts
FCC first ideas

## Slide 3: The aim: 16 T, 20 T (+ ?) for high energy colliders
Present studies for future high energy hadron colliders:
FCC-hh at CERN, two options under study
  100 TeV (com) in a 80 km ring with 20 T dipole magnets (baseline)
  100 TeV (com) in a 100 km ring with 16 T dipole magnets
  The FCC study was launched in February 2013
SppC Qinhuangdao China 50-90 TeV (com) in a 50-70 km ring (20T-16 T) but concentrating on the e+e- option at the moment

## Slide 4: Some possible FCC-hh geometries
LHC
27 km, 8.33 T
14 TeV (c.o.m.)
FCC-hh
80 km, 20 T
100 TeV (c.o.m.)
FCC-hh
100 km, 16 T
100 TeV (c.o.m.)
HE-LHC
27 km, 20 T
33 TeV (c.o.m.)

## Slide 5: FCC-hh main ring
For the FCC-hh main ring many new magnet types will be needed
Below are listed the very preliminary ideas for the 16 T option
 | B / G (T) / (T/m) | Bpeak (T) | Bore (mm) | Length (units x m)
MB | 16 | 16.4 | 50 | 4500 x 14.3
MQ | 450 | 13 | 50 | 800 x 6
MQX | 225 | 13 | 100 | tbd
D1 | 12 | 13 | tbd | 4x2 x 12
D2 | 10 | 10.5 | tbd | 4x3 x 10

## Slide 6: Conductors for high field accelerator magnets
The needs:
In order to attain high fields in a geometry that is practical in a tunnel:
Je should be >400A/mm2 (B prop. to width of coil and Je)
To have a good (<few units 10-4) ‘dynamic’ field quality the cable should be multi-filamentary to limit eddy currents
To keep the magnet “protectable” in case of a quench
Je should be <600A/mm2 (limiting the energy density per volume of coil)
I cable should be >10kA (limiting the voltage at fast ramp-down and hence the inductance)

## Slide 7: Conductors for FCC
16 T option
Nb3Sn: (non-Cu part)
  Jc 2000 A/mm2 @ 15 T & 1.9 K
Jc 1400 A/mm2 @ 15 T & 4.2 K
20 T option
HTS:
  Je 600 A/mm2 @ 20 T & 1.9 K (B perpendicular)
Nb3Sn: (non-Cu part)
  2000 A/mm2 @ 15 T & 1.9 K
1400 A/mm2 @ 15 T & 4.2 K

## Slide 8: Available superconductors: Jc
(critical current density
in the superconductor Jc)

## Slide 9: Available superconductors: Je
(Engineering critical current density Je)

## Slide 10: Nb3Sn conductor Jc development
ITER
US-CDP
CARE-NED
EuCARD
HL-LHC
HL-LHC specs
FCC
FCC specs

## Slide 11: Nb3Sn strands
Nb3Sn for High Field Magnets
examples
OST (US)
  Restacked Rod Process (RRP) for High Energy Physics (r= 0.7 mm or 0.8 mm, Jc up to 3000 A/mm2@12T, 4.2 K, filaments~50 mm, Cu-nonCu=0.9)
EAS-Bruker (De)
  Powder in Tube (PIT) for HEP and others (r=1 mm, Jc up to 2400 A/mm2@12T , 4.2 K, filaments ~50 mm, Cu-nonCu=1.25)
To be reacted at 650°C for ~120 hr

## Slide 12: Nb3Sn Conductor for HEP
Courtesy L. Bottura, B. Bordini
0.7 mm, 108/127 stack
RRP from Oxford OST
1 mm, 192 tubes
PIT from Bruker EAS
Between HL-LHC and FCC the Jc target shifts from 12 T to 16 T !

## Slide 13: Nb3Sn cables for the CERN HFM Program
SMC Dipole cable – 14 strands (1.25 mm) and
18 Strands (1 mm), Width = 10 mm, Twist Pitch = 60 mm
Average IC degradation 0 … 4 %
DS Dipole cable – 40 Strands (0.7 mm)
Width = 14.7 … 15.1 mm, Twist Pitch = 100 mm, 0.8° keystone
Average IC degradation < 3 %
Fresca 2 Dipole cable – 40 Strands (1 mm)
Width = 20.9 mm, Twist Pitch = 120 … 140 mm
Average IC degradation < 15 %
Cabling by L. Oberli and A. Bonasia (CERN)
Cabling tests were performed on several variants of strands/cable sizes to explore the space of parameters, and among others: dimensions, compaction, twist pitch, cabling angle and cabling force, …
Cabling degradation was reduced from 45 % (worst case) to negligible (within the scatter of measurements of extracted strands)

## Slide 14: Superconducting tapes: YBCO
YBCO: Yttrium barium copper oxide
Available in tapes : YBCO deposited on a substrate to impose the texture (1-2 mm)
Can reach > 600 A/mm2 (overall) but serious issue is the anisotropy
Is strong under axial stress and strain
Limited cabling possibilities:
Difficult technology but could be promising for high field magnets in >18 T region.
A

## Slide 15: Superconducting strands and tapes: BSCO
BSCO: Bismuth strontium calcium copper oxide
Available in strands (OST)
Can reach 400 A/mm2 (overall)
Is fragile under stress and strain
Powder in a silver tube
Has to be reacted at 850°C with a temperature precision of 1°C in an oxygen atmosphere
Can be cabled in high current Rutherford cables
Difficult technology but could be promising for high field magnets in >20 T region

## Slide 16: The magnet challenge beyond 10 T
HL-LHC will be a first for Nb3Sn magnets in accelerators and an intermediate step towards the future machines
FCC

## Slide 17: Comparison between dipoles and solenoids
We can see roughly a factor 2 due to Coil «efficiency» and to force-stress management

## Slide 18: The magnet challenge beyond 10 T
Nb-Ti : blue diamonds, nominal field
Nb3Sn: red squares, maximum field
As a rule magnets are used with ~20% margin (nominal = 0.8 x maximum)
Existing magnets for machines and test models

## Slide 19: Forces (and mechanics)
The electromagnetic loads in a 20 T dipole would be a factor 5 to 8 larger than in the LHC dipole
Scaling of force on coil quadrant in recent production and R&D dipoles
The supporting shell for a 15T-class magnet, with apologies to J.-C. Perez, CERN
x 5

## Slide 20: Around and beyond 10 T before 2004
Already for the LHC in 1986 Nb3Sn was considered an option for the 10 T magnets which were then foreseen. The magnet by Asner-Perin 1987 went up to 9.5 T at 4.2 K. Many problems though remained in the manufacturing.
In 1995 Twente constructed the MSUT that was powered up to 11 T.
For the VLHC studies FNAL designed the HDFA magnet series that attained 9.4 T (@4.2 K)
The D20 magnet of LBNL (still) has the field record in a dipole aperture at 13.8 T. With the HD1 LBNL reached 16 T in a 8 mm aperture (much too small for an accelerator)
Texas A&M ( P. McIntyre) is working on a block coil dipoles with ‘stress management’

## Slide 21: LHC IP Quadrupole design and technology evolution
70
90
120
150
Aperture (optics)
Courtesy L. Bottura

## Slide 22: LARP: Ten years of intense R&D
Subscale Quadrupole
SQ
0.3 m long
110 mm bore
2004-2006
Technology Quadrupole
TQS - TQC
1 m long
90 mm bore
2006-2010
Long Quadrupole LQS
3.7 m long
90 mm bore
2007-2012
High Field Quadrupole HQ
1 m long
120 mm bore
2008-2014
Long Racetrack LRS
3.6 m long
No bore
2006-2008
LQS01
LQS03
HQ01b-c
HQ01d-e
HQ02
TQS01
LRS01
SQ02
Courtesy G. Sabbi & H. Felice

## Slide 23: US dipole R&D, LBNL
Since 20 years LBNL is running a high field dipole development program
Some achievements:
D20, 50 mm aperture, cosQ 4 layer dipole, reached 12.5 T
HD1, flat block coil, 8 mm aperture, reached 16 T
HD2, flared end block coil, 36 mm aperture, reached 13.8 T
These pose a clear breakthrough abode 10 T with a new coil layout (block coil) and a new mechanical structure (shell-bladder and keys) aimed at high fields
Courtesy, P. Ferracin, LBNL
D20

## Slide 24: LBNL block coil designs
Block coil
  Used with thick coils the field quality is good
    Not yet used in accelerators
  Is less efficient (~10%) wrt to cos(Q) for quantity of superconductor used
  The EM forces cause a stress buildup at the outside edge of the coil where the fields are lower
  The straight part is very easy : rectangular cable and wedges (field quality)
  ‘flared ends’ look easy but there is little experience exists to make them
HD2
Courtesy LBNL

## Slide 25: High Field Magnet development program in Europe
Some history of HFM development in Europe
2004-2008 FP7-CARE-NED project (Next European dipole)
  Development of European accelerator grade Nb3Sn conductor  Powder In Tube (PIT) conductor now available from Brucker
  Various studies on design options and materials
2009-2013 PF7-EuCARD-HFM project (High Field Magnets)
  Development of a 100mm aperture 13 – 15 T Nb3Sn dipole “Fresca2”
  Development of an HTS insert with DB = 6 T (inside Fresca2)
  Development of an HTS current link
  Development of a Nb3Sn helical undulator
2008 – 2014 CERN High Field Magnet project
  Development of Nb3Sn technology magnets for LHC upgrades and new projects (conductor, small models, materials, etc)

## Slide 26: High Field Magnet development program at CERN
Present structure of the HFM development
Present – 2016 HL-LHC (HILUMI) HFM magnet development
  140 T/m 150 mm aperture low beta Nb3Sn quadruple (QXF) (LARP-CERN collaboration)
  11T Nb3Sn dipole for dispersion suppressor (FNAL-CERN collaboration)
2014 – 2017 FCC study
  Design study for 16 T dipole
  Design study for 20 T dipole
2013 – 2017 FP7- EuCARD2- MAG (Future Magnets)
  Development of 10kA HTS cable for accelerator magnets
  Development of an accelerator quality 5 T HTS dipole

## Slide 27: HL-LHC: MQXF low beta Nb3Sn quadrupole magnet
A CERN LARP collaboration.
Nominal Gradient 140 T/m Aperture diameter 150 mm
Peak Field 12.1 T
Current 17.5 A
Loadline Margin 20% @ 1.9 K
Stored Energy 1.32 MJ/m

## Slide 28: HL-LHC: MQXF low beta Nb3Sn quadrupole magnet
Both in at US-LARP and CERN first coils are under construction:
First magnet test at FNAL with US and CERN coils in 2nd half 2015

## Slide 29: HL-LHC: 11 T Dispersion suppressor magnet
First Nb3Sn magnet to go into an accelerator (2018) !
Present model program (CERN and FNAL)
  demonstrating the required performance (11.25 T at 11850 A) and Achieve accelerator field quality
NOTE: virtual reality model
FNAL MBHSP02 ready for test
By courtesy of D. Mitchell, F. Nobrega (FNAL) and M. Karppinen (CERN)
CERN coil
Nominal Field 11 T
Aperture diameter 60 mm
Peak Field 11.35 T
Current 11.85 kA
Loadline Margin 19.7% @ 1.9 K
Stored Energy 0.96 MJ/m

## Slide 30: HL-LHC: 11 T Dispersion suppressor magnet
CERN first model: attained 11T
FNAL several models tested: attained 11T
Complete feasibility to be shown this year at CERN with 2m models (field, field quality,
Meanwhile long magnet construction being set up.
The first 2 units to be installed in LS2 in DSs of IP2
This will be the first Nb3Sn magnet to be used in an accelerator: important prove of concept for the future

## Slide 31: EuCARD high field dipole FRESCA2: Nb3Sn dipole magnet for cable test facility
Nominal Field 13 T
Aperture diameter 100 mm
Peak Field 13.2 T
Current 10.7 A
Loadline Margin 20% @ 4.2 K
Stored Energy 3.6 MJ/m

## Slide 32: EuCARD high field dipole (Fresca2)
Diameter Aperture = 100 mm
L coils = 1.5 m
L straight section = 700 mm
L yoke = 1.6 m
Diameter magnet = 1.03 m
156 turns per pole
Iron post
Bcenter = 13.0 T
I13T = 10.7 kA
Bpeak = 13.2 T
Emag = 3.6 MJ/m
L = 47mH/m
Courtesy Attilio Milanese, Pierre Manil
42
42
36
36
Fresca2 : CERN, CEA construction phase
First tests end 2015

## Slide 33: FRESCA2: Nb3Sn dipole magnet for cable test facility
Cu coil layer 1-2 reacted
Cu coil layer 3-4 impregn.
Coil fabrication

## Slide 34: FRESCA2: Nb3Sn dipole magnet for cable test facility
Qualification with dummy coil completed after 3 pre-loads and cool-downs
Support structure

## Slide 35: SMC/RMC: race track development magnets
RMC (Racetrack Model Coil)
Laminated Yoke
Vertical Pad
Aluminium Shell
Longitudinal Rods
Horizontal Pad
Nb3Sn Coil
Electrical connexion box
SMC (Short Model Coil)
Short Model Coil
FReSCa2
Nb3Sn Dipole
Race-track
Model Coil

## Slide 36: SMC/RMC: race track development magnets
Test results SMC 11T #2
RMC mechanical assembly
RMC finished coil
RMC coil winding
RMC coil ready for reaction

## Slide 37: EuCARD, 6 T insert
B0 = 6 T
Je= 250 A/mm2
Bpeak= 5,87 T
Inom = 2400 A
3 double layers coils
External tube, Nitronic 40
- 8 parts,
- Thermal shrinkage
- TIG welding
External pads, 316L
8/9 parts, Electron-beam
welded
Iron pole
Compression plates, 316L
Contact
Contact
Hastelloy + sc (65 mm)
460 mm
Hastelloy + sc (65 mm)
Cuopper 70 mm
CuBe2 + polyester insulation (100 + 30 mm)
130 µm
200 mm
12 mm (nominal)
CuBe2 + polyester insulation (100 + 30 mm)
130 mm
Electron-beam welding
After a long development phase the assembly is starting now
First stand alone test Q3 2015
Test in Fresca2 outsert end 2016
Insert conductor is composed of three tapes

## Slide 38: EuCARD2: 5T HTS dipole
YBCO HTS, 40 mm clear aperture, 5 T in stand alone & 17 T in Fresca2 dipole background field
Angular dependent cable
Current distribution
Roebel tape cable 10 kA
High Force Structure
Short Sample in
different position
Cable aligned with field
Aligned coil block dipole

## Slide 39: Explotring new ideas: Aligned coil block dipole
PhD work Jeroen van Nugteren

## Slide 40: Alternative EuCARD2 dipole designs
Courtesy: John Himbele (CNRS- Grenoble)
JE = 400 A/mm2
Block with stacked tapes YBCO cable
Courtesy: Clément Lorin (CEA)
Cosine-Theta with YBCO cable

## Slide 41: FCC : Strawman coil design for 16 T and 20 T
From: E. Todesco, IEEE TAS, 24(3), 2014, 4004306
15 T “Snowmass” design
4578 units (+ 160 spares)
1000 tons of LHC-grade Nb-Ti
3500 tons of HEP-grade Nb3Sn
20 T “Malta revised” design
3662 units (+ 120 spares)
1000 tons of LHC-grade Nb-Ti
3000 tons of HEP-grade Nb3Sn
750 tons of HTS
16 T Nb3Sn block (2014)

## Slide 42: Coil configuration for 20 T
Scan of possible configurations with YCBO-Nb3Sn-Nb-Ti grading (Thesis J. van Nugteren)

## Slide 43: New (old) design very suitable for Bi-2212 (LBNL, FNAL…)

## Slide 44: Conclusions
There is an active High Field accelerator Magnet R&D program running in Europe and the US
The principle aim is to prepare for FCC, a 100 TeV hadron-hadron collider
Two main development road are being pursued for FCC
  16 T dipoles
  20 T dipoles
Development of HF quadrupoles is being defined at the moment
HL-LHC is also to be seen to show the feasibility for accelerator magnets >10T; ie. with Nb3Sn instead of Nb-Ti conductor
Exciting times ahead !